Contingency Casing Design

If hole conditions dictate, 7" casing will be set at 7 233' MD (6,960' TVD) A 6 1/8" hole will then be drilled to 11 375' MD (6,960' TVD) where 4 1/2" casing will be set and cemented with one stage up to dv tool. After completion procedures, the 4 1/2" casing will be cut and pulled at 6400'

2nd Intermediate

|  | 0 ft to 100 ft | Make up Torque ft-lbs | Total ft = 100 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| O D | Weight | Grade | Threads | opt min | mx |  |
| 7 inches | 26 #/ft | J-55 | LT&C | 3670 | 2750 | 4590 |
| Collapse Resistance | Internal Yield | Joint Strength | Body Yield | Drift |  |  |
| 4,320 psi | 4,980 psi | 367 ,000 # | 415 ,000 # | 6.151 |  |  |

|  | 100 ft. to | 5,800 ft | Make up Torque ft-lbs | Total ft = | 5,700 |
| --- | --- | --- | --- | --- | --- |
| O D | Weight | Grade | Threads | min | mx |
| 7 inches | 23#/ft | J-55 | LT&C | 3130 | 2350 |
| Collapse Resistance | Internal Yield | Joint Strength | Body Yield | Draft |  |
| 3,270 | 4,350 psi | ...:313,000# | 366,000# | 6.25 |  |

|  | 5,800 ft to | 7,233 ft | Make up Torque ft-ibs | Total ft = | 1,433 |
| --- | --- | --- | --- | --- | --- |
| O.D | Weight | Grade | Threads | min | mx |
| 7 inches | 26 #/ft | J-55 | LT&C | 3670 | 2750 |
| Collapse Resistance | Internal Yield | Joint Strength | Body Yield | Dnft |  |
| $ 4,320^{{psi}} $ | 4,980 psi | 367,000 # | 415,000 # | 6,151 |  |

Lead w/760sx Lite crete (YLD 2 66 Wt 9 9) tail w/125sx PVL (YLD 1 41 Wt 13) TOC = Surface

Production

|  | 0 ft to 11,375 ft | Make up Torque ft-lbs | Total ft = 11,375 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| O D\n4.5 inches | Weight\n11.6 #/ft | Grade\nHCP-110 | Threads\nLT&C | opt\n3020 | min\n2270 | mx\n3780 |
| Collapse Resistance\n8,650 psi | Internal Yield\n10,690 psi | Joint Strength\n279 ,000 # | Body Yield\n367 ,000 # | Dnft\n3.875 |  |  |

UV tool placed at approx 6400' and cemented with one stage up to UV tool. After completion procedures, the

4 1/2" casing will be cut and pulled at 6400'.